Olzhas Kurikov

[ok34@hw.ac.uk](mailto:ok34@hw.ac.uk)

**Resonant Ultrasound Spectroscopy**

Analysis of thickness resonances to characterise a material

Master Thesis Project

16.01.2017 – 03.07.2017

Supervisor

Prof. Marc Desmulliez

Second supervisor

Prof. Thomas Speck

Co-supervisor

Dr. Anne Bernassau

Heriot-Watt University, Edinburgh

Albert-Ludwig’s University, Freiburg

1. **Introduction**

The aim of this project was to establish reliable setup to characterise a living material using resonant ultrasound spectroscopy. In the first stage of the project, the solid materials such as aluminium, glass and plastics were tested to prove that setup is well tested and ready to switch to a living materials such as plants. The experiments were performed with aluminium, glass and plastic due to existing elastic constants, hence it is straightforward to compare datasheet values to analysed data.

The main reason why exactly ultrasound resonant spectroscopy was used is that that by measuring transmission coefficient of a sample, RUS can infer parameters like thickness, density, attenuation coefficient, speed of sound and first order resonant frequency. Moreover, this technique is non-destructive and non-invasive. Therefore, there is no damage on a sample which is significantly important for a plant samples, while running the experiment.

Coefficient of transmission of sound at normal incidence through each sample in the frequency range 0.6 MHz – 1.7 MHz was measured. For all cases, at least one thickness resonance was observed. From these measurements density, sound velocity, and attenuation of ultrasonic longitudinal waves were obtained and compared to available data provided in an articles or by manufacturers.

The method is based on frequency-domain analysis, by using the Fast Fourier transform, of pulse transmitted through a sample.

All the experiments were conducted in Biology department of Albert-Ludwig’s University of Freiburg city in Germany. And the required equipment, except oscilloscope (listed below) were transported from Heriot-Watt University, Edinburgh:

* Transducer
* Hydrophone
* Water tank
* Pulser/receiver
* DC coupler
* Oscilloscope

Results reveal that these resonances are strongly sensitive on different parameter changes which are discussed further in the report.

This report goes through all the steps and problems which are faced during the experiments and gives suggestions for further improvements.

1. **Literature review and theory**
   1. **Fundamentals of ultrasound**